## Slide 1: Plasmonic Transistors For Terahertz-band Communication
Dr. Jonathan Bird
(Professor & Chair
Department of Electrical Engineering)
Aarbaj Mundaganur
Shahabaj Mundaganur
November 3rd 2023

## Slide 2
Demand for High-Speed, High-Bandwidth Data Communication
Source: Trotman, Andrew & Zhang, Jinglan. (2013). Future Web Growth and its Consequences for Web Search Architectures.
In January 2023, 5.16 billion people worldwide had internet access.
In just the past five years, we've seen an additional 1.2 billion users join this community.
With increase in internet users, consequently the demand for higher data rates will continue to increase.
Note: Data sourced from the 'Digital 2023: Global Overview Report' by Simon Kemp, dated 26 January 2023.
We are here
~5 Billion
2023
~8 Billion

## Slide 3
Evolution of Communication Networks
Chart: Data Rate (Kilobit per sec)
| 1974 | 1991 | 1998 | 2008 | 2019 | 1G | 2G | 3G | 4G | 5G
Data Rate | 2.4 | 64 | 2000 | 100000 | 1000000
2.4 Kbit/s
64 Kbit/s
2 Mbit/s
100 Mbit/s
1 Gbit/s

## Slide 4
Exploring Terahertz Spectrum for Next Generation Communication Schemes
Wavelength | Absorption | Energy | Penetration
3 mm to 30 um | Strongly absorbed by water & organic substances | Low energy, Non-ionizing radiation | High penetration compared to visible light

## Slide 5
Our Primary Objective
To develop high speed, compound semiconductor based plasmonic transistors suitable for next generation of communication schemes.
These devices will operate at THz frequencies.

## Slide 6
Dyakonov and Shur Instability For Plasma Wave Oscillations
Pioneering work done by Dyakonov and Shur in 21 June 1993.
Asymmetric boundary conditions required for the plasma waves growth under DC drain bias.
Adapted from M Dyakonov, M Shur Phys. Rev. Lett. 71, 2465 (1993)

## Slide 7
Our Plasmonic Device Design
Theoretical study of a semiconductor field-effect transistor designed with a dual grating gate.
Plasma oscillations in the individual elementary cells are coupled to one another via EM interaction.
A drastic enhancement of the radiated EM power should occur due to coherent addition of the EM waves generated in different cells.
Notes: Periodic modulation of the 2D electron channel leads to the formation of a plasmonic crystal.

## Slide 8
DS Instability in Plasmonic Asymmetric Gate Array Device
A fringing capacitance is formed between the 2D electron layer and the gate edge.
The fringing capacitances will be different at the opposite edges of this gate.
Cb= αεε0W
Asymmetric Factor = γ = Cb2 / Cb1 > 1
(Cb2 ≠ Cb1)
Equivalent electric circuit diagram of the gate array

## Slide 9
Theoretical Model
α = Geometric factor
β = Ratio of e- density (n01/n02)
γ = Asymmetric factor
M = Mach number = v0/vp
ω = Plasma frequency
.
Hydrodynamic equations based on Dyakonov and Shur shallow water analogy
electron-fluid density () and
velocity ()
We solve this dispersion equation for as a function of k.

## Slide 10
Theoretical Model Simulations
Considerations for the simulation
InGaAs-based TeraFET
0.042
nm,
3 × 1011 cm-2, =3,
0.05,
~2 THz

## Slide 11
Experimental progress requirement
Electron Beam Lithography Scanning Electron Microscopy
Focused Ion Beam Scanning Electron Microscope
(FIB-SEM) - Carl Zeiss AURIGA CrossBeam
E-Beam Lithography System (100kV)
Elionix ELS-G100

## Slide 12
Experimental update on plasmonic device fabrication
Source
Drain
Gate I
Gate II
Mesa Etch
Mesa Etch
Recess Etch
25 µm

## Slide 13
Process Flow for Our Plasmonic Device Fabrication
Step | Instrument/ Process | Purpose
1 | EBL | Markers Exposure
2 | E-Beam Evaporator | Markers Metal deposition
3 | EBL | Mesa Exposure
4 | Wet Chemical Etching | Mesa Etch
5 | Citric Acid Etching | Leakage Prevention Etch
Step | Instrument/ Process | Purpose
6 | EBL | Gate recess exposure
7 | Wet Chemical Etching | Gate recess etch
8 | EBL | Gate array exposure
9 | E-Beam Evaporator | Gate array metal deposition
10 | EBL | Contact pads exposure
11 | E-Beam Evaporator | Contact pads metal deposition

## Slide 14
20 µm
Harsh proximity effect
Gate array exposure trials
Gate Array Design
Proximity Error Correction Map

## Slide 15
Reducing the total resist layer thickness
(From 500 nm to 220 nm )
2.Minimizing beam current during EBL exposure. Beam Current = 100 pA
3. Running dose test to identify optimal exposure dose.
4. Maximizing the scanning dot resolution for the EBL to 1,000,000 dots.
Investigation into reducing proximity error
Previous Stack
New Stack

## Slide 16
10 µm
No harsh proximity effect
Gate Array Design Trial
Proximity Error Correction Map
20 µm
Harsh proximity effect
After optimizing proximity correction

## Slide 17
Asymmetric Gate Array Trial
(nm)
(Diagram is for representational purpose only and the scales are in nm)
10 µm
230 nm
Dose
460 uC/cm2
Dose
470 uC/cm2
Gate Width
50 um

## Slide 18
Gate Width
50 um
Optimized Design
Dose
675 uC/cm2
GaAs Substrate
200 nm
Shorting between gates
Dose Increase

## Slide 19
Gate Height 50 um
Dose 700 uC/cm2
Exp. Design
150-150-30-270
Approx. Measurement
180-120-55-240
Metal Thickness Decreases
Dose Increase
GaAs Substrate
1 µm

## Slide 20
SEM image of an asymmetric gate array pattern fabricated on our heterostructure substrate using EBL
600 nm

## Slide 21
Potential Misalignment Issue
Misalignment
Misalignment
Optical microscope images displaying alignment issues with gate array and recess
Device Failure
14 µm
14 µm
100 µm

## Slide 22
Accurate Alignment using Pre-fabricated Markers
6 X 6 Matrix of Markers (500 um apart)

## Slide 23
The optical microscope image of a marker with 100x magnification
SEM image of a marker center
Step 1 and 2: Results
100X
5 µm
500 nm

## Slide 24
Step 3: Mesa Isolation Exposure
EBL Parameters | 
Field Size | 500 um
Exposure Current | 20nA
Exposure Dose | 1000 uC/cm2
Number of Dots | 50,000
Resist Layers/ Thickness | A4-A5/ 500 nm
Optical microscope image of mesa exposure after development with 10x magnification
Development : 35 sec MIBK: IPA =1:3
10X
60 µm

## Slide 25
Step 4: Wet Chemical Etching
Etching Parameters:
•The clean room temperature: 65.70 F
•The speed of magnetic stirrer: 400 rpm
•Initial mixing time: 10 min
•Chemicals used:
1. Phosphoric acid (H3PO4) 85+% solution in water
2. Hydrogen peroxide (H2­O2) 30%
3. Deionized Water (H2O)
•Ratio used: 1:1:40
•Amount used: 3 ml : 3 ml : 120 ml •Etching time: 125 seconds.
InP based InGaAs Heterostructure used in this work

## Slide 26
Step 4: Mesa Etching
Step 5: Citric Acid Etching
Result
Optical microscope image after mesa etch and citric acid etching with 10x magnification
10X
Note: It can be seen that the bottom surface after the etching process is not uniform at some regions. However, the isolation still holds true, as evident after etch depth measurement.
60 µm

## Slide 27
Step 6: Gate Recess Exposure
Optical microscope image after recess exposure
60 µm
10X
Conducting

## Slide 28
Step 7: Gate Recess Etch
Similar etching recipe used from step 4 except for the etching time.
Etching Time = 15s
Optical microscope image after gate recess etching
100X
4 µm
Etched

## Slide 29
Step 8 and 9: Asymmetric Gate Array Exposure, Metal Deposition, and Liftoff
EBL Parameters | 
Field Size | 500 um
Exposure Current | 100pA
Exposure Dose | 820 uC/cm2
Number of Dots | 1,000,000
Resist Layers/ Thickness | A4-A2/ 250 nm
Development : 35 sec MIBK: IPA =1:3

## Slide 30
Step 8 and 9: Results
Optical microscope images after gate array exposure (Left) and after metal liftoff (Right)
(Metal deposited
Cr/Au:5/25 nm)
100X
100X
4 µm
4 µm

## Slide 31
Step 10 and 11: Results
10X
50X
On the left is a 10X optical-microscope image of our plasmonic gate array device, after the last step in the process flow i.e., after the contact pad metal deposition (Cr/ Au: 10/ 150 nm) and lift-off. The figure on the right is a 50X optical-microscope image of the center part of our plasmonic gate array device.
25 µm
150 µm

## Slide 32
100 µm
Practice device
inspection using SEM

## Slide 33
Practice device
inspection using SEM
2 µm

## Slide 34
Practice device
inspection using SEM
1 µm

## Slide 35
Practice device
inspection using SEM
1 µm

## Slide 36
Practice device
inspection using SEM

## Slide 37
Practice Device Inspection
using SEM
200 nm

## Slide 38
Wire Bonding
8 x 5 mm

## Slide 39
Next Steps
Perform electrical testing on the fabricated devices, and measure transistor performance.
Systematic analysis of gate array design on plasma wave growth.
Comprehensive device characterization, involving measurements for contact resistance (TLM measurements), mobility, mean free path, electron density (Hall bar measurements)

## Slide 40
Paper and Conference Presentations
B. Barut, X. Cantos-Roman, J. Crabb, A. Mundaganur, S. Mundaganur, T. Sugaya, E. Einarsson, J.M. Jornet, J.P. Bird, and G.R. Aizin, “Asymmetrically engineered nanoscale transistors for on-demand sourcing of terahertz plasmons”, contributed talk, the 22nd International Conference on Electron Dynamics in Semiconductors, Optoelectronics and Nanostructures (EDISON22), Munster, Germany, August 14th – 18th, 2023.
G. Aizin, S. Mundaganur, A. Mundaganur, and J. P. Bird, “Terahertz-frequency plasmonic-crystal instability in field-effect transistors with asymmetric gate arrays”, submitted for publication.
A. Mundaganur and S. Mundaganur, and J.P. Bird, “Asymmetrically engineered nanoscale transistors for on-demand sourcing of terahertz plasmons”, poster presentation, Workshop on Innovative Nanoscale Devices and Systems (WINDS 2023), Hawaii, USA, December 3rd–8th, 2023.

## Slide 41: THANK YOU!

## Slide 42
Supplementary Slides

## Slide 43
T. Otsuji, M. Shur, IEEE Microwave Magazine, Volume:15, Issue:7, Nov.-Dec. 2014
THz Devices

## Slide 44
Frequency Type | Frequency Range | Common Uses
Very High Frequency | 30 MHz to 300 MHz | FM radio, television broadcasting, mobile radio, air traffic control
Ultra-high Frequency | 300 MHz to 3 GHz | Mobile networks (4G), Wi-Fi, Bluetooth, GPS
Super High Frequency | 3 GHz to 30 GHz | Satellite communications, Mobile networks (5G)
Extremely High Frequency | 30 GHz to 300 GHz | Radio astronomy, remote sensing, research and development
Communication Bands

## Slide 45
Dyakonov- Shur Instability experiments and their limitations
      Physically shorting the source to the gate and driving the transistor into saturation.
Customized HEMT designs in which the gate was positioned closer to the source than the drain were fabricated.
      Precise placement of nanoscale gate near etched trench at the drain side of the plasmonic device. (Research done in our lab)
Boundary conditions satisfied for DS instability.
Still, the radiated power was expected to be very weak (~nW) for practical applications.

## Slide 46
Alignment Achievement Using Marker Design
Total marker alignment process count = 4 (Step 3,6,8, and 10)
Alignment tolerance threshold achieved ~ 20nm
Example:

## Slide 47
Step 5: Citric Acid Etching
Etching Parameters:
•The clean room temperature: 65.70 F
•The speed of magnetic stirrer: 400 rpm
•Initial mixing time: Until Citric Acid dissolves completely
•Chemicals used: 1. Citric acid (C6H8O7)
2. Hydrogen peroxide (H2­O2) 30%
3. Deionized Water (H2O)
•Ratio used: - 2gr : 1ml : 2ml
•Amount used: - 20 gr : 10 ml : 20 ml
•Etching time: 60 seconds.

## Slide 48
Step 10 and 11: Contact Pads Pattern Exposure, Metal Deposition, and Liftoff
EBL Parameters | 
Field Size | 500 um
Exposure Current | 20nA
Exposure Dose | 1000 uC/cm2
Number of Dots | 50,000
Resist Layers/ Thickness | A4-A5/ 500 nm
Development : 35 sec MIBK: IPA =1:3
E beam Evaporator Parameters | 
Vacuum Pressure | 5E-7 Torr
Bottom Layer Deposition Rate | 0.5 Angstrom/s
Top Layer Deposition Rate | 0.8 Angstrom/s
Bottom Layer Metal Film | Cr (10 nm )
Top Layer Metal Film | Au(150 nm)

## Slide 49
Practice device
inspection using SEM
2 µm