## Slide 1: High-Energy-Density All-Solid-State Batteries with Sulfur-Based Electrolytes
Hedi Yang & Jaehee Park
PI: Prof. Ying Shirley Meng
05/10/2024
Mini-Conference
Engineering Nano-Scale Structures for Advanced Applications

## Slide 2
Atomic-level
Electronic-level
Single Particle-level
Meso-structure-level
Electrode-level
20 μm
Funded by
US Department of Energy (2010 – present)
US National Sciences Foundation (2010 – present))
EFRC – NCCESS (2010-2020)
Battery500 (2016 – present)
LGES Frontier Research Laboratory (2021 – present)
Various Industrial Partners including
(LG Energy Solution / ThermoFisher Scientific / Shell / UL /Nissan /Cummins/ SES/ Supernal /GM / Applied Materials)
Science 2015
Science 2017 (South 8 Technologies, Inc)
Nature Energy 2018
Joule 2018, 2020
Nature 2019
Nature Nanotechnology 2020 (Unigrid, Inc)
Nature Materials 2020
Nature Energy 2021
Science 2021
Joule 2022 (ExPost Technologies Inc.)
Nature Nanotechnology 2023
Three Spun Out Startup Companies
Eight Issued Patents and Ten Pending
Workforce from Meng Group
2010 – 2023
30 + 9 Postdoctoral
40 + 20 Ph.D.
14 + 1 Master
23 + 6 Undergraduate
Atom to System - Build Talents, Ideas and An Ecosystem
Notes: Dr. Y. Shirley Meng is a Professor at the Pritzker School of Molecular Engineering at the University of Chicago. She serves as the Chief Scientist of the Argonne Collaborative Center for Energy Storage Science (ACCESS) Argonne National Laboratory. Dr. Meng is the principal investigator of the research group - Laboratory for Energy Storage and Conversion (LESC), that was established at University of California San Diego since 2009. She held the Zable Chair Professor in Energy Technologies at University of California San Diego (UCSD) from 2017-2022. Dr. Meng received several prestigious awards, including ECS Battery Division Research Award (2023), the C3E technology and innovation award (2022), the Faraday Medal of Royal Chemistry Society (2020), International Battery Association IBA Research Award (2019), Blavatnik Awards for Young Scientists Finalist (2018), C.W. Tobias Young Investigator Award of the Electrochemical Society (2016) and NSF CAREER Award (2011). Dr. Meng is elected Fellow of Electrochemical Society (FECS), Fellow of Materials Research Society (FMRS) and Fellow of American Association for the Advancement of Science (AAAS). She is the author and co-author of more than 300 peer-reviewed journal articles, two book chapters and eight issued patents. She is the Editor-in-Chief for Materials Research Society MRS Energy & Sustainability. Dr. Meng received her Ph.D. in Advance Materials for Micro & Nano Systems from the Singapore-MIT Alliance in 2005. She received her bachelor’s degree in Materials Science with first class honor from Nanyang Technological University of Singapore in 2000

## Slide 3
Hedi Yang
2nd year graduate student at the Pritzker School of Molecular Engineering (PME) at the University of Chicago
Yang has been a member of Meng group since his undergraduate and Master’s studies at UCSD and is trained extensively on the basic techniques and procedures of solid-state battery materials. Yang’s contributions in Dr. Darren Tan et al.’s article1 on carbon-free Si anodes for solid-state batteries provides him with sufficient theoretical and practical knowledge on the topic.
Jaehee Park
1st year graduate student at the Pritzker School of Molecular Engineering (PME) at the University of Chicago
Park has been a member of the Meng group, bringing her solid-state battery expertise developed during her master‘s studies at Kyoto University and further honed through her work on lithium dendrite challenges. Her proficiency is highlighted by her research using operando X-ray computed tomography, notably published2 in this field. At Meng group, Park has been extensively trained in both sulfide and halide-based SSE materials, building on a strong foundation in material synthesis—covering solid-state electrolytes, sulfur/Li2S-based cathodes, and micro-Si anodes—and basic electrochemical characterization of LiIn-Li2S cells.
1Science 373.6562 (2021): 1494-1499.; 2Chem. Commun., 2023, 59, 7799
Project Members

## Slide 4
Global CO2 emissions driven by economic and population growth ( > 40 Gt CO2/yr)
Projected increase in electricity demand ( > 1000 TWh)
Electric vehicles and renewable energy push for better batteries
Reliability of renewables
Electrification for efficiency
Increase renewable fuel share
IPCC, 2014: Climate Change 2014: Synthesis Report, U.S. Battery Market Size And Share, Industry Report, 2030
Growing Demand for High-Capacity Batteries

## Slide 5
Li-S batteries can cause a paradigm shift for currently inaccessible technologies
InfoMat. 2022 4(9), e12359; Adv. Mater. 2020, 2003955
Why Sulfur?
10th most abundant
Parameter | Intercalation-Type Cathodes | Conversion-Type Cathodes
Reaction Mechanism | Ion insertion into layered structure | Full material transformation
Energy Density (Wh/kg) | Up to 260 | Up to >260*, conditional
Theoretical Capacity (mAh/g) | 100-265 | 500-1675
Cost Effectiveness | Moderate | Potentially lower, abundant sulfur
Example | Commercialized cathode LiCoO2 | S, FeF2
Note: *It can with specific conditions such as lean electrolyte, high areal capacity, and high sulfur loading.
Advantages of Conversion-Type Li-S Batteries

## Slide 6
Mater. Chem. Front., 2023, 7, 5760–5785
Liquid electrolyte Solid-state electrolyte
Multi-step conversion
1st stage: S8→Li2Sn
(2.2 to 2.3 V)
2nd stage: Li2Sn → Li2S
(2.0 to 2.1 V)
Soluble lithium polysulfides
Shuttle effect
Electrolyte leakage
Dendrite growth
Reliance on solid-solid contact
Ionic/electronic conduction
(Electro)chemical stability
Mechanical properties
Impact of Electrolyte Evolution on Battery Performance

## Slide 7
ACS Cent. Sci. 2020, 6, 7, 1095–1104; Chem. Mater.2020, 32, 360−373
Bottlenecks of liquid Li-S
Polysulfide dissolution
Insulative properties
Sluggish kinetics
Benefits of solid electrolyte
Resolve polysulfide dissolution
Inert against chemical degradation by polysulfides
Structural integrity
All-Solid-State Battery: Solution for Polysulfide Dissolution

## Slide 8
Advanced Energy Materials 10.1: 1903253; ACS Energy Lett. 2019, 4, 2418−2427
High ionic conductivity (>1 mS/cm at RT)
Provides ionic conduction pathways
Suitable voltage window (~2 V vs. Li/Li+) for Li-S (2.1 -2.4 V)
Phosphorous
Sulfur
Lithium
Chlorine
Decomposition products are
Redox active (Reversible reaction)
Stabilize the cathodic interface
Li6PS5Cl (LPSCl)
Benefits of LPSCl in Solid-State Li-S Batteries

## Slide 9
  This project aims to develop the conversion-based S cathode system to further improve the performance of next generation solid-state LIBs. The objective of the second year is to utilize the skills obtained prior such as
    Material synthesis
    Sample preparation & data analysis for novel characterization methods
    ASSB fabrication & cycling evaluation
  to evaluate & optimize the novel material system.
Research Statement (Second Year)

## Slide 10
Proposed Metric | Baseline (1st Year) | Mid Project (2nd year) | End Project (3rd year)
Energy Density | - | > 250 Wh/kg | > 350 Wh/kg
Cycle life | 100 (> C/3, <20%) | 500 (> C/3, < 20%) | 1000 (> C/3)
Critical current | > 5 mA/cm2 | > 7 mA/cm2 | > 10 mA/cm2
1st CE | > 75% | > 80% | > 85%
Avg CE / Cycle | > 99% | > 99.5% | > 99.9%
Areal Capacity | > 4 mAh/cm2 | > 5 mAh/cm2 | > 6 mAh/cm2
Operating Pressure | < 50 MPa | < 25 MPa | < 5 MPa
Temperature | Room Temp | Room Temp | -20 to 80
Proposed Metric | Baseline (1st Year) | Mid Project (2nd year) | End Project (3rd year)
Energy Density | - | > 250 Wh/kg | > 350 Wh/kg
Cycle life | 100 (> C/3, <20%) | 500 (> C/3, < 20%) | 1000 (> C/3)
Critical current | > 5 mA/cm2 | > 7 mA/cm2 | > 10 mA/cm2
1st CE | > 75% | > 80% | > 85%
Avg CE / Cycle | > 99% | > 99.5% | > 99.9%
Areal Capacity | > 4 mAh/cm2 | > 5 mAh/cm2 | > 6 mAh/cm2
Operating Pressure | < 50 MPa | < 25 MPa | < 5 MPa
Temperature | Room Temp | Room Temp | 
Research Statement (Second Year)

## Slide 11
System Overview & Synthesis Procedure
Material Qualification & Characterization
Cycling Data
Presentation Workflow

## Slide 12
One-step sulfur cathode composite synthesis
Li1In1 synthesis
Schematic & Procedural Credit: Ashley Cronk
Cathode Composite
Sulfur : LPSCL : Acetylene Black
30 wt% 50 wt% 20 wt%
Cell holder schematic
Sintering Pressure: 375 MPa
Stack Pressure: 75 MPa
Advanced Energy Materials 10.1 (2020): 1903253.
SLMP
In Powder
Li + In = Li1In1
Vortex-mixed until even
Batteries & Supercaps 2.6 (2019): 524-529.
“Triple-phase contacts”
Reduce complexity
Enhances scalability
Retained active surface
System Overview and Synthesis Procedure

## Slide 13
Milled S Composite
+
+
=
SEM Stub
(Side View)
SEM Stub
(Top View)
Carbon
Tape
Powder
Sample
SEM
Sample
Composite components (LPSCl, S, C)
  Low/similar atomic mass nuclei
  Difficult to distinguish contrast
EDX also provide little information
  P & Cl distribution did not show discrete LPSCl vs S/C particles
Requires other methods of investigation
Sample prepared by Jerry Yang; Images collected by Dr. Sam Oh
SEM & EDX to Probe Particle Morphology

## Slide 14
Sample prepared by Jerry Yang; Spectra collected by Ashley Cronk
Nature Reviews Methods Primers 1.1 (2021): 21.
Airtight Raman sample prepared using kapton tape and microscope cover slide
LPSCl clear PS43− peak at 425.4 cm−1
S Cathode Composite PS43− contribution vanishes  reduction of symmetry
Shift in low wavenumber S peak
  red shift, indicates formation of polysulfidophosphates
Cover
slide
Powder
sample
Kapton
Tape
Raman
Sample
+
+
=
Raman Spectroscopy to Investigate Chemical Bonding

## Slide 15
Bragg’s Law
Interplanar spacing for cubic system
Powder
sample
Capillary Tube
+
Temporarily Sealed Capillary
Blow
Torch
Capillary
XRD Sample
=
+
=
Airtight XRD Sample prepared using Capillary tubes
LPSCl characteristic peaks
S characteristic peaks
S cathode composite
  Large amorphous hump from carbon contribution
  Signals from S & LPSCl characteristic peaks
Sample prepared by Jerry Yang; Spectra collected by Phillip Ridley
X rays and crystal structure. Bell, 1915.
X-ray Diffraction to evaluate Crystallographic Information

## Slide 16
S Composite
Ti
Ti
Material | Resistance (Ω) | Electronic Conductivity (S/cm)
LPSCl | - | 4.95×10-9
S | - | 5×10-30 (literature)
S Composite | 5.620 | 5.89×10-3
Used the low voltage stimulus of 30, 60, 90 mV to minimize electrochemical reaction between the materials
Incorporation of carbon in the composite significantly increase the electronic conductivity
Conductivity Equation
V = IR
Ohm’s Law
ACS Sustainable Chemistry & Engineering 8.32 (2020): 12100-12109.
DC Polarization to probe electronic conductivity

## Slide 17
Cell Type: Solid-state Half Cell
Cycling Protocol: 0.375V – 2.375V
Cathode Loading: 2.5 mg S Composite
Anode Loading: 50 mg Li1In
Current Density: C/20
Operating Conditions: 100 MPa, RT
Li1In
S Composite
1.6 mAh/cm2
Loading (mAh cm-2) | 1st DC (mAh/g) | 1st C (mAh/g) | ICE% | Conversion Efficiency
1.6 | 1549.2 | 1966 | 126.9% | 97.3%
Capacity values exceeds theoretical values (1675 mAh g-1)
  Electrolyte contributing to capacity
Single plateau reaction  different from liquid Li-S
Decrease in polarization after initial formation cycle
High capacity-retention at high C rates
Cycling Evaluation of S Cathode vs Li1In (1.6 mAh cm-2)

## Slide 18
Cell Type: Solid-state Half Cell
Cycling Protocol: 0.375V – 2.375V
Cathode Loading: 9 mg composite
Anode Loading: 100 mg Li1In
Current Density: C/20
Operating Conditions: 100 MPa, RT
Li1In
S Composite
1.6 mAh/cm2
Loading (mAh cm-2) | 1st DC (mAh/g) | 1st C (mAh/g) | ICE% | Conversion Efficiency | Polarization at 50% C/DC
1.6 | 1549.2 | 1966 | 126.9% | 97.3% | 0.5677 V
5.5 | 1446.1 | 1814.2 | 125.5% | 97.3% | 0.6638 V
5.5 mAh/cm2
Similar C/DC capacity value & curve shape
Increase in voltage polarization at 50% C/DC
Retain similar performance at >5 mAh/cm-2
0.5677 V
0.6638 V
Li1In
Cycling Evaluation of S Cathode vs Li1In (5.5 mAh cm-2)

## Slide 19
Proposed Metric | Baseline (1st Year) | Mid Project (2nd year) | End Project (3rd year)
Energy Density | - | > 250 Wh/kg | > 350 Wh/kg
Cycle life | 100 (> C/3, <20%) | 500 (> C/3, < 20%) | 1000 (> C/3)
Critical current | > 5 mA/cm2 | > 7 mA/cm2 | > 10 mA/cm2
1st CE | > 75% | > 80% | > 85%
Avg CE / Cycle | > 99% | > 99.5% | > 99.9%
Areal Capacity | > 4 mAh/cm2 | > 5 mAh/cm2 | > 6 mAh/cm2
Operating Pressure | < 50 MPa | < 25 MPa | < 5 MPa
Temperature | Room Temp | Room Temp | -20 to 80
Proposed Metric | Baseline (1st Year) | Mid Project (2nd year) | End Project (3rd year)
Energy Density | - | > 250 Wh/kg | > 350 Wh/kg
Cycle life | 100 (> C/3, <20%) | 500 (> C/3, < 20%) | 1000 (> C/3)
Critical current | > 5 mA/cm2 | > 7 mA/cm2 | > 10 mA/cm2
1st CE | > 75% | > 80% | > 85%
Avg CE / Cycle | > 99% | > 99.5% | > 99.9%
Areal Capacity | > 4 mAh/cm2 | > 5 mAh/cm2 | > 6 mAh/cm2
Operating Pressure | < 50 MPa | < 25 MPa | < 5 MPa
Temperature | Room Temp | Room Temp | 
Research Baseline & Metrics

## Slide 20
Acknowledgements
LESC
The work was initiated in the collaboration project with LGES with two patents pending
Paper Submission
  Cronk et al., A highly utilized and practical lithium sulfur cathode realized with sulfide solid electrolytes. Submitted. (2024)
II-VI Foundation

## Slide 21
Thank You for Listening!
Questions and Answers?